The SEP force field model

The parameter values are estimated (but not exclusively) from the MM2, TraPPE force field, and Weiner et al..

Stretching

U = ks/2 (lb-r)2

C–C	lb=1.5 Å	ks=4404 kg s-2 (J/m) (634 kcal mol-1 Å-2)
C=C	lb=1.33 Å	ks=7920 kg s-2 (J/m) (1140 kcal mol-1 Å-2)
C-C (aromatic)	lb=1.41 Å	ks=616 kg s-2

In MM2 (Allinger, 1977) ks/2 for type 1 is listed as 317 kcal mol-1 Å-2. Aromatic parameters are simply average of double and single bond parameters (Weiner et al, JACS, 1984).

Bending

Harmonic U = kθ /2 (θ-θ0)2
Cosine squared U = kθ /2 (cos(θ)-cos(θ0))2

C-C-C	θ0 = 109o	kθ=8.62 ·10-19 J (124 kcal mol-1 rad-2)
C-C-C (aromatic)	θ0 = 120o	kθ=9.72 ·10-19 J (139 kcal mol-1 rad-2)

The values are optimized for harmonic potential. Have been used for cosine squared with success.

Torsion

U = c0 + c1cos(φ) + c2cos2(φ) + c3cos3(φ) + c4cos4(φ) + c5cos5(φ) [Ryckaert-Belleman]

C-C-C-C (alkane)	Ryckaert-Belleman
C-C-C-C (zero angle)	c1 = 6.90 ·10-19 J (15 kcal mol-1 rad-2) other zero
C-C-C-C (180 angle)	c1 = -6.90 ·10-19 J (-15 kcal mol-1 rad-2) other zero

Charges

X-[C]1-[O]2-[H]3	q1=0.265, q2=-0.700, q3=0.435